Weekly Meeting
CCI
6 Aug 2024

---
Progress Summary
Fixed some structures
DFT!!!
As always, complications
- Began DFT calculations
- Looked at DFT scripts, ran bulk relaxations with DFT and progressing to slab energies
- started with single point, moving on to Esurf
- STO looks a lot better now
- Overall, confident in enough structures to proceed with workflow
     - MBEEF and VDW. Wasn’t including dispersion effects so we changed to ‘MGGA_X_MBEEFVDW’
- Learning further about Slurm

---
111 Surfaces - STO

---
111 Bulk – Testing varying Kgrid values
Potential E	CPU Time	Difference (Ev)
Kgrid 222
-185323.079	50.998	0.304
Kgrid 333
-185323.384	51.265	0.00682
Kgrid 433
-185323.390	51.076	0.00598
Kgrid 443
-185323.396	51.027	0.00508
Kgrid 444
-185323.401	50.941	0.00643
Kgrid 555
-185323.408	50.779	0.00129
Kgrid 666
-185323.409	51.827	0.000471
Kgrid 777
-185323.410	52.515	-

---
DFT with 111 Surfaces - ST
Nlayers	CPU time	Eslab (single)
3	69.894	-555608.226
4	108.384	-740812.271
5	150.811	-926016.313
6	214.785	-1111220.355
7	270.932	-1296424.397
8	331.965	-1481628.439
9	436.599	-1666832.481
10	496.688	-1852036.523

---
DFT with 111 Surfaces - ST
N Layers	Esurf
3	5.986
4	7.954
5	?

---
Currently in Progress
100 Surfaces
- ST
  Running until Esurf converges
- STO & Py
  Getting started on single points and running calculations to get relaxed energies of slab
111
- Oterm and Cuterm
  Single point calculations
- 3011
  This is a crucial surface but I am really not sure where to begin here

---
Future Work – 100 Surfaces 3011
- Papers Cu36 and O18
- Mine with 3 layers Cu36 and O18

---
Future Work – 100 Surfaces 3011