Weekly Meeting
CCI
16 July 2024

---
Progress Summary
Completing MACE Calculations
Hawk
Finding issues
- Colab’s usage limits
- Created python scripts of notebooks and running on Hawk’s GPUs
- Convergence issues, switched to MDMin rather than LBFGs
- Half of the results are reasonable, half given negative Esurf
- Py111 is getting stuck on Hawk at same point
- 3011

---
111 Surfaces - CuD
Number of Layers	Number of Oxygen Atoms	Surface Energy
3	6	0.15416508443751
4	8	0.183357653680009
5	10	0.352855734115526
6	12	0.346735474351216
7	14	0.230233310666001
8	16	0.296124771050448
9	18	0.346855030919947
10	20	0.22638172801723

---
111 Surfaces - STO
3	17	-0.89473429434951
4	23	-1.19924660179911
5	29	-1.51698125223084
6	35	-1.88952778122397
7	41	-2.22161903540179
8	47	-2.52544844020025
9	53	-2.88493624351716
10	59	-3.21663130296169

---
100 Surfaces - Oterm
3	6	0.217057754797947
4	8	0.238842434934108
5	10	0.217130908792016
6	12	0.238851209372439
7	14	0.333070469351174
8	16	0.238865206707302
9	18	0.217131593010626
10	20	0.393892033967003

---
100 Surfaces - c2x2
3	8	-0.344793316862565
4	12	-1.02176404901413
5	18	-1.63689048363973
6	18	-1.45254819345539
7	24	-2.06768823714255
8	26	-2.31414604179933
9	32	-2.92928313606701
10	34	-3.17570040521406

---
Next Steps - 3011
- Remake supercell with (2,-1,1,1)
- Compare surface energies of mine and theirs

---
Next Steps - DFT

---
111 Surfaces - ST
3	17	-0.89473429434951
4	23	-1.19924660179911
5	29	-1.51698125223084
6	35	-1.88952778122397
7	41	-2.22161903540179
8	47	-2.52544844020025
9	53	-2.88493624351716
10	59	-3.21663130296169